Plastics Guidelines

The following guidelines are presented for those machinists not familiar with the machining characteristics of plastics. They are intended as guidelines only, and may not represent the most optimum conditions for all parts. The troubleshooting quick reference in this section should be used to correct undesirable surface finishes or material responses during machining operations.

Most quality stock shape materials are stress relieved to ensure the highest degree of machinability and dimensional stability. However, the relative softness of plastics (compared to metals) generally results in greater difficulty maintaining tight tolerances during and after machining. A good rule of thumb for tolerances of plastic parts is +/- .001 per inch of dimension although tighter tolerances are possible with very stable, reinforced materials.

When machining plastic stock shapes, remember...

- Thermal expansion is up to 10 times greater with plastics than metals

- Plastics lose heat more slowly than metals, so avoid localized overheating

- Softening (and melting) temperatures of plastics are much lower than metals

- Plastics are much more elastic than metals

Because of these differences, you may wish to experiment with fixtures, tool materials, angles, speeds and feed rates to obtain optimum results.

Getting Started

- Positive tool geometries with ground peripheries are recommended

- Carbide tooling with polished top surfaces is suggested for optimum tool life and surface finish. Diamond coated or polycrystalline tooling provides optimum surface finish when machining Duratron® XP or Vespel® PI or Celazole* PBI.

- Use adequate chip clearance to prevent clogging

- Adequately support the material to restrict deflection away from the cutting tool

Turning
Operations require inserts with positive geometries and ground peripheries. Ground peripheries and polished top surfaces generally reduce material build-up on the insert, improving the attainable surface finish. A fine grained C-2 carbide is generally best for turning operations.

Drilling
The insulating characteristics of plastics require consideration during drilling operations, especially when hole depths are greater than twice the diameter.

Small diameter holes (232" or 1mm to 1.0 or 25mm)
High speed steel twist drills are generally sufficient for small holes. To improve swarf removal, frequent pull-out (peck drilling) is suggested. A slow spiral (low helix drill will allow for better swarf removal.

Large diameter holes (1.0” or 25mm and larger)
A slow spiral (low helix) drill or general purpose drill bit ground to a 118° point angle with 9° to 15° lip clearance is recommended. The lip rake should be ground (dubbed off) and the web thinned.

It is generally best to drill a pilot hole (maximum 1/2” diameter) using 600 to 1,000 rpm and a positive feed of 0.005” to 0.015” per revolution. Avoid hand feeding because of the drill grabbing which can result in microcracks forming. Secondary drilling at 400 to 500 rpm at 0.008 to 0.020” per revolution is required to expand the hole to larger diameters.

A two step process using both drilling and boring can be used on notch sensitive materials such as Ertalyte® PET-P, Torlon* PAI, Duratron® XP, Vespel® PI, Celazole* PBI and glass or carbon reinforced products. This minimizes heat build-up and reduces the risk of cracking.

- Drill a 1” diameter hole using an insert drill at 500 to 800 rpm with a feed rate of 0.005” to 0.015” per revolution.

- Bore the hole to final dimensions using a boring bar with carbide insert with 0.015” to 0.030” radii at 500 to 1,000 rpm and a feed rate of 0.005 to 0.010” per revolution.

Threading and Tapping
Threading should be done by single point using a carbide insert and taking four to five 0.001” passes at the end. Coolant usage is suggested. For tapping, use the specified drill with a two flute tap. Remember to keep the tap clean of chip build-up. Use of a coolant during tapping is also suggested.

Milling
Sufficient fixturing allows fast table travel and high spindle speeds when end milling plastics. When face milling, use either high positive or high shear geometry cutter bodies

Sawing
Band sawing is versatile for straight, continuous curves or irregular cuts. Table saws are convenient for straight cuts and can be used to cut multiple thicknesses and thicker cross sections up to 4” with adequate horsepower. Saw blades should be selected based upon material thickness and surface finish desired.

- Rip and combination blades with a 0° tooth rake and 3° to 10° tooth set are best for general sawing in order to reduce frictional heat.

- Hollow ground circular saw blades without set will yield smooth cuts up to 3/4” thickness.

- Tungsten carbide blades wear well and provide optimize surface finishes.

Coolant Recommendations

Coolants are generally not required for most plastic machining operations (not including drilling and parting off). However, for optimum surface finishes and close tolerances, non-aromatic, water soluble coolants are suggested. Spray mists and pressurized air are very effective means of cooling the cutting interface. General purpose petroleum based cutting fluids although suitable for metals and some plastics, may contribute to stress cracking of amorphous plastics such as Acrylic, Polycarbonate, Polysulfone, Ultem® PEI, and Radel® R PPSU.

Coolants Tips

- Coolants are strongly suggested during drilling operations, especially with notch sensitive materials such as Ertalyte® PET-P, Torlon® PAI, Duratron® XP, Vespel® PI, Celazole® PBI and glass or carbon reinforced products.

- In addition to minimizing localized part heat- up, coolants prolong tool life. Example (flood) coolants suitable for most plastics include:

  - Cimstar 40B (CimCool Milacron, Cincinnati, OH)

  - Trim 9106CS (Master Chemical, Perrysburg, OH)

  - Polycut (Tullco, Savannah, GA).

A generally suitable mist coolant is Astro-Mist 2001A (Monroe Fluid Technology, Hilton, NY).

FABRICATION GUIDELINES - TURNING AND DRILLING MATERIALS REL. MACHIN- ABILITY (1 to 10 1=easiest) TURNING DRILLING** Depth of cut Speed Feet/Min. Feed, In./Rev. Nominal Hole Dia. Feed, In./Rev. Acetal copolymer Delrin®, Delrin® AF Delrin® AF Blend Nylon 101 Nylatron® GS, GSM Nylatron® GSM Blue Nylatron® NSM MC® 901, MC® 907 Nylon Polycarbonate Polysulfone Ultem® 1000 & 2300 PEI 1 1 1 1 1 1 1 1 3 3 7 .150” .025” 500-600 600-700 .010-.015 .004-.007 1/16" 1/8" 1/4" 1/2" 3/4" 1" 1 1/2" 2" or > .007-.015 " " .015-.025 " .020-.050 " " Fluorosint® 500 Fluorosint® 207 1 1 .150” .025” 350-500 500-600 .010-.015 .003-.008 1/16" 1/8" 1/4" 1/2" 3/4" 1" 1 1/2" 2" or > .007-.015 " " .015-.025 " .020-.050 " " PEEK™, unfilled PEEK 30% GF PEEK 30% CF 5 7 7 .150” .025” 600-1000 600-700 .010-.016 .004-.007 1/16" 1/8" 1/4" 1/2" 3/4" 1" 1 1/2" 2" or > .002-.005 " " .004-.008 " .008-.012 " " Ertalyte® PET-P Ertalyte® TX Hydex® 4101 PBT-P .150” .025” 500-600 600-700 .010-.015 .004-.007 1/16" 1/8" 1/4" 1/2" 3/4" 1" 1 1/2" 2" or > .002-.005 " " .015-.025 " .020-.050 " " Techtron® PPS Ryton® PPS Ryton® BG PPS .150” .025” 100-300 250-500 .010-.020 .005-.010 1/16" 1/8" 1/4" 1/2" 3/4" 1" 1 1/2" 2" or > .007-.015 " " .015-.025 " .020-.050 " " Torlon® 4203 PAI Torlon® 4301 PAI Torlon® 4501 PAI Torlon® 4503 PAI Torlon® 4540 PAI Torlon® 5530 PAI Duratron® XP Vespel® PI .025” 300-800 .004-.025 1/16" 1/8" 1/4" 1/2" 3/4" 1" 1 1/2" 2" or > .007-.015 " " .015-.025 " .020-.050 " " Celazole® PBI .150” .025” 100-150 150-225 .005-.010 .002-.006 1/16" to 1/4" 1/2" or > .005-.015 .015-.025

FABRICATION GUIDELINES - MILLING MATERIALS End Milling / Slotting Face Milling (C-2) Carbide Tool high speed steel (m2,M7) Depth of cut Speed, ft./min. Feet, in./tooth Depth of cut Speed, ft./min. Feet, in./tooth Acetal copolymer Delrin 150, Delrin AF Delrin AF Blend Nylon 101 Nylatron® GS Nylon Nylatron® GSM, Nylatron® GSM Blue, Nylatron® NSM MC® 901 Nylon, MC® 907 Nylon 1/4" 1/2" 3/4" 1", 2" 1/4" 1/2" 3/4" .250 " " " .050 " " 270-450 " " " 300-500 " " 0.002 0.003 0.005 0.008 0.001 0.002 0.004 0.150 0.060 1300-1500 1500-2000 0.020 0.005 Polycarbonate Polysulfone Ultem® 1000 PEI Ultem® 2300 PEI 1/4" 1/2" 3/4" 1", 2" 1/4" 1/2" 3/4" .250 " " " .050 " " 270-450 " " " 300-500 " " 0.002 0.003 0.005 0.008 0.001 0.002 0.004 0.150 0.060 1300-1500 1500-2000 0.020 0.005 PEEK™ 1/4" 1/2" 3/4" 1", 2" 1/4" 1/2" 3/4" .250 " " " .050 " " 270-450 " " " 300-500 " " 0.002 0.003 0.005 0.008 0.001 0.002 0.004 0.150 0.060 500-750 " 0.020 0.005 Fluorosint® 500 Fluorosint® 207 1/4" 1/2" 3/4" 1", 2" 1/4" 1/2" 3/4" .250 " " " .050 " " 270-450 " " " 300-500 " " 0.002 0.003 0.005 0.008 0.001 0.002 0.004 0.150 0.060 500-700 550-750 0.010 0.005 Techtron® PPS Ryton® PPS 1/4" 1/2" 3/4" 1", 2" 1/4" 1/2" 3/4" .250 " " " .050 " " 270-450 " " " 300-500 " " 0.002 0.003 0.005 0.008 0.001 0.002 0.004 0.150 0.060 1300-1500 1500-2000 0.020 0.005 Torlon® PAI 1/4" 1/2" 3/4" 1", 2" 1/4" 1/2" 3/4" .250 " " " .050 " " 270-450 " " " 300-500 " " 0.002 0.003 0.005 0.008 0.001 0.002 0.004 0.035 500-800 .006-.035 Ertalyte® PET-P Ertalyte® TX Hydex® 4101 PBT-P 1/4" 1/2" 3/4" 1", 2" 1/4" 1/2" 3/4" .250 " " " .050 " " 270-450 " " " 300-500 " " 0.002 0.003 0.005 0.008 0.001 0.002 0.004 0.150 0.060 1300-1500 1500-2000 0.020 0.005 Duratron® XP Vespel® PI Celazole® PBI 1/4" 1/2" 3/4" 1", 2" 1/4" 1/2" 3/4" .50 .015 450-650 " " " 250-350 " " 0.005 0.002 0.050 0.015 450-650 250-350 0.005-.010 .002-.006

FABRICATION GUIDELINES - SAWING MATERIALS Sawing Material thickness Tooth form Pitch teeth/in. Band Speeds ft./min. Acetal copolymer Delrin 150, Delrin AF Delrin AF Blend Nylon 101 Nylatron® GS Nylon Nylatron® GSM, Nylatron® GSM Blue, MC® 901 Nylon, MC® 907 Nylon <1/2" 1/2"-1" 1"-3" 3" Precision " Butress " 10-14 6 3 " 3,000 2,500 2,000 1,500 Polycarbonate Polysulfone Ultem® 1000 PEI Ultem® 2300 PEI <1/2" 1/2"-1" 1"-3" 3" Precision " Butress " 10-14 6 3 " 4,000 3,500 3,000 2,500 PEEK™ <1/2" 1/2"-1" 1"-3" 3" Precision " Butress " 8-14 6-8 3 " 4,000 3,500 3,000 2,500 Fluorosint® 500 Fluorosint® 207 <1/2" 1/2"-1" 1"-3" 3" Precision " Butress " 8-14 6-8 3 " 3,000 2,500 2,000 1,500 Techtron® PPS Ryton® PPS <1/2" 1/2"-1" 1"-3" 3" Precision " Butress " 8-14 6-8 3 " 5,000 4,300 3,500 3,000 Torlon® PAI <1/2" 1/2"-1" 1"-3" 3" Precision " Butress " 8-14 6-8 3 " 5,000 4,300 3,500 3,000 Ertalyte® PET-P Ertalyte® TX Hydex® 4101 PBT-P <1/2" 1/2"-1" 1"-3" 3" Precision " Butress " 10-14 6 3 " 5,000 4,300 3,500 3,000 Duratron® XP Vespel® PI Celazole® PBI 3/8"-1" 1"-2" Precision " Butress " 10 10 3,000 1,500

TROUBLESHOOTING QUICK REFERENCE Drilling Difficulty Common Cause Tapered hole 1. Incorrectly sharpened drill 2. Insufficient clearance 3. Feed too heavy Burnt or melted surface 1. Wrong type drill 2. Incorrectly sharpened drill 3. Feed too light 4. Dull drill 5. Web too thick Chipping of surfaces 1. Feed too heavy 2. Clearance too great 3. Too much rake (thin web as described) Chatter 1. Too much clearance 2. Feed too light 3. Drill overhang too great 4. Too much rake (thin web as described) Feed marks or spiral lines on inside diameter 1. Feed too heavy 2. Drill not centered 3. Drill ground off-center Oversize holes 1. Web too thick 2. Insufficient clearance 3. Feed rate too heavy 4. Point angle too great Undersize holes 1. Dull drill 2. Too much clearance 3. Point angle too small Holes not concentric 1. Feed too heavy 2. Spindle speed too slow 3. Drill enters next piece too far 4. Cut-off tool leaves nib, which deflects drill 5. Web too thick 6. Drill speed too heavy at start 7. Drill not mounted on center 8. Drill not sharpened correctly Burr at cut-off 1. Dull cut-off tool 2. Drill does not pass completely through piece Rapid dulling of drill 1. Feed too light 2. Spindle speed too fast 3. Insufficient lubrication from coolant Cutting Off Melted surface 1. Dull tool 2. Insufficient side clearance 3. Insufficient coolant supply Rough finish 1. Feed too heavy 2. Tool improperly sharpened 3. Cutting edge not honed Spiral marks 1. Tool rubs during its retreat 2. Burr on point of tool Concave or convex surfaces 1. Point angle too great 2. Tool not perpendicular to spindle 3. Tool deflecting (use negative rake) 4. Feed too heavy 5. Tool mounted above or below center Nibs or burrs at cut-off point 1. Point angle not great enough 2. Tool dull or not honed 3. Feed too heavy Burrs on outside diameter 1. No chamfer before cut-off 2. Dull tool Turning & Boring Melted surface 1. Tool dull or heel rubbing 2. Insufficient side clearance 3. Feed rate too slow 4. Spindle speed too fast Rough finish 1. Feed too heavy 2. Incorrect clearance angles 3. Sharp point on tool (slight nose radius required) 4. Tool not mounted on center Burrs at edge of cut 1. No chamfer provided at sharp corners 2. Dull tool 3. Insufficient side clearance 4. Lead angle not provided on tool (tool should ease out of cut gradually, not suddenly) Cracking or chipping of corners 1. Too much positive rake on tool 2. Tool not eased into cut (tool suddenly hits work) 3. Dull tool 4. Tool mounted below center 5. Sharp point on tool (slight nose radius required) Chatter 1. Too much nose radius on tool 2. Tool not mounted solidly 3. Material not supported properly 4. Width of cut too wide (use 2 cuts)