How and Why 3D Prints Fail
Causes
Symptoms
Cures

---
Print Failure Causes
- Print Doesn’t Stick to the Bed
- Communication Failure Between Computer and Printer
- Filament Runs Out
- Filament tangles on spool
- Print layers shifting
- Bad GCODE
- Extruder problems
- Bad Filament
- SD Card Problems

---
Print Doesn’t Stick to the Bed
- The most common cause of print failure
- Many possible causes include:
  - Bed or extruder too cool
    - Print first layer hot
  - Bed dirty
    - Clean it before starting a print
  - Nozzle too high or too low for first layer
    - Learn how to adjust it
  - Bed not level
    - Learn how to adjust it
  - First layer printed too fast
    - Print first layer slowly – 20-30 mm/sec
  - Model footprint too small
    - Use brim or raft and/or support material to ensure adequate footprint
  - Over or under extrusion of filament
    - filament diameter set in slicer should match the diameter on the spool
  - Wrong bed surface material
    - Use material that plastic likes to stick to
      - PEI or Kapton
  - Forgot gluestick (specific to CubePro Trio printer at MMS)

---
Communication Failure
- Many possible causes
  - Computer goes to sleep
  - Computer reboots for security update
  - Flaky USB driver
  - USB cable problems
    - Cat chews through cable
    - Cable pulled out mid-print
    - Bad connector at computer or printer or cable
  - Someone decides to play video game while a print is running
  - Computer falls on the floor while a print is running
  - Someone turns off computer while a print is running
- One solution: print from SD card

---
Filament Runs Out During Print
- Printer stops completely or stops extruding when there’s no filament
  - Slicers provide filament usage estimate for print
  - Know how much filament is on the spool before you start a print
    - Weigh filament spool and subtract empty spool weight

---
Filament Tangles on Spool
- Filament ties itself into a knot and extruder stops extruding
- 98% of the time, this is a user problem
  - don’t let free end of filament loose when loading, unloading, and storing filament
  - don’t use vertical axis spool holders
  - Store filament with the free end threaded through holes in the spool flanges
- 2% of the time, filament jumps over flanges of spool
  - Use a spool holder design that doesn’t let that happen

---
Print Layers Shifting
- Usually happens in the Y axis of printers that move the bed in the Y axis
  - Caused by motor losing control of the mechanism due to inertia of the bed
    - Reduce acceleration and jerk or junction deviation in controller firmware to regain control
    - Increase motor current to increase torque
  - SoM specific: can be caused by mechanical resonance
    - Keep all speeds <= 40mm/sec

---
Bad GCODE
- Inappropriate slicer settings- a user problem
  - know the printer and filament you’re using
  - set appropriate slicer options for your print
- Slicer problem- incomplete GCODE file
  - specifically slic3r problem with SD cards
  - make sure the card isn’t full before you export GCODE- slic3r won’t warn you
- Always review slicer settings and check print layer view before exporting GCODE, then check GCODE file after exporting it to SD card.

---
Extruder Problems
- Jamming
  - Usually a temperature issue
    - Hot end cooling fan should be running at all times
    - Make sure hot-end temperature is high enough
    - Rarely, foreign object finds its way into the hot-end
      - Requires disassembly of hot-end to fix
    - Retraction length should be short (usually <2mm) in direct extruders
    - Can occur if hot-end temperature varies widely
      - Check thermistor and cable
- Extruder drive gear chewing divots into the filament
  - Should never happen
    - increase pinch roller pressure so drive gear teeth bite deeply into the filament
- Can’t feed flexible filament- filament bunches up or winds around the extruder drive gear
    - Slow print speed to 20-30 mm/sec max for all layers
    - Decrease pinch roller pressure
    - Minimize use of or disable retractions
This should NEVER happen!

---
Bad Filament
- Usually PLA
- Multiple failure modes
  - Filament brittle, breaks easily
    - Improper storage- moisture absorption
  - Bubbles in print surface, hissing/popping while extruding
    - Improper storage- moisture absorption
    - Store the filament in a dry box with desiccant
    - Preferred method is a gasketed plastic box with a tub of DampRid (CaCl) desiccant.
  - Poor filament quality- poorly controlled diameter
    - Jams at entrance to extruder or run-out sensor
      - Buy better filament next time

---
SD Card Problems
- Corrupt file system
  - Always “eject” SD card from computer before pulling it out of the slot
- Too big card- printer can’t read files
  - Use low capacity cards (<=2GB) formatted using FAT file system
- Card incompatible with printer, or card is dead
  - Rare, but it happens, try a different card
- mSD card used with adapter not working
  - Not always reliable, best to avoid use
- Slic3r specific problem- incomplete gcode file on the card
  - Make sure the card has adequate room before you export GCODE- slic3r won’t warn you if the card fills before the GCODE is stored
  - Check the GCODE file for completeness after export
    - Slic3r stores print settings at the end of the gcode file- look for them with a text editor

---
Save Yourself a Lot of Heartache
- Store filament properly
  - Dry bag or box with desiccant - CaCl better than silica gel
  - Thread the loose end of filament through holes in spool flange
  - Use filament up in a timely manner- PLA seems to have a limited shelf life.
- Handle filament properly
  - Always keep control of the loose end when loading and unloading spools from printer
- Weigh new spools and mark empty spool weight on every spool
- Measure filament diameter in 20-30 places and calculate average diameter. Mark average diameter on spool flange and use it when you slice or print.
- Before starting a print, if there’s any doubt about sufficient filament on the spool, weigh it.