Designing Parts to be 3D Printed
Basic Considerations

---
Print Strength
- Prints are made in layers
  - Result is anisotropic strength
- Orientation on the print bed matters
  - Strongest in tension in X and Y, compression in Z
  - Weakest in tension in Z and compression in X and Y
- Forces that try to split or shear the bond between layers do the most damage
  - Screws driven into sides of prints can split layers
- If you need strength and/or rigidity
  - Make prints chunky
  - Use high fill density
  - Select strong fill pattern
  - Use multiple perimeters and multiple top and bottom solid layers
  - Use wide lines to maximize layer to layer contact area
  - Use a large nozzle diameter (allows wider lines)
  - Print hot to ensure strong layer to layer bonds
- Choose the right filament material for the application

---
Use of Support Material
- Support enables steeply overhanging parts to be printed
- Support not usually needed for bridges
- Generated automatically in the slicer when you enable the option
  - Different slicers generate different support
  - Multiple settings available to customize the support for the print
- Some downsides to the use of support
  - Uses more filament
  - Increases print time
  - Poor first layer over support quality
  - Removal usually leaves scars on the print
- Design for minimal use of support
  - Orientation on the bed matters
    - But don’t forget about strength
  - Make sure support material will be accessible for removal
  - Design your object as multiple parts to be printed without support and joined after printing
- Use fingers, wire cutter, needle nosed pliers, and razor knife to remove support material from print
  - Be careful- plastic fragments, especially PLA, and tools can be very sharp

---
Support Material
- Support needed for overhanging print structures
  - Varies a little with filament and print settings
- Note the horizontal split in the forehead
  - This is what happens when you print ABS in an open printer
That’s support material under the noses and chins

---
No Support Material Needed
- If the overhanging structures aren’t too horizontal, they can be printed without support material
  - Print quality can suffer on the underside of the overhanging structure.

---
Detail Sizes in Your Object
- Smallest convex details (think teeth of a comb) can be no smaller than the extruder nozzle diameter
  - Use a small nozzle for finer detail
    - Slower to print – requires thinner layers, more perimeters, more top and bottom solid layers
    - Weaker prints due to small contact area between layers
    - Very small nozzles jam easily
- Smallest concave details (think of the space between the teeth of a comb) can be arbitrarily small
  - Limited by printer XY resolution, extruder calibration, quality of linear motion components, and printer frame rigidity
- Thinnest walls no thinner than one printed line width (usually extruder nozzle diameter)

---
Holes
- Horizontal holes in vertical walls can be printed without support
  - Usually a little small due to roughness of the outline, and sagging plastic at the top of the hole
- Vertical holes in prints are always smaller than designed in CAD
  - STL is a polygonal approximation of a circle
  - Plastic shrinks as it cools, pulling it inward, toward the center of the hole
- How to deal with it
  - In CAD, make holes 0.2-0.4 mm larger (experimentation required)
  - If holes are small, use a drill bit to open holes to final size after printing

---
Designing Prints to Mate With Other Objects
- Other object(s) may be printed or not
- Start your design by modeling the other object(s)
  - Download a CAD model from the manufacturer, if possible
    - Also check McMaster-Carr
  - Use a caliper to make measurements
  - Use only as much detail as needed
- Design the print object around the model of the other object(s)
  - Allow a few 1/10ths of a mm for clearances
    - Make simple, quick-to-print test pieces to check sizes
  - Use modifier meshes (slicer option) to increase infill density around screw holes

---
Modeling

---
Make a Test Print
This print was used
to test the spacing
of the gears’ axles
to ensure the gears
would mesh properly
- Know what you want to test
  - Design a simple part that will print quickly

---
Modeling

---
Designing Prints to Mate With Other Prints
- Use registration pins to align parts to be joined
  - Make the hole slightly larger diameter than the pin
- Design for threaded brass inserts for screws that require frequent removal and replacement
- Design for through-bolts
  - Use modifier mesh to ensure solid plastic under nut and screw head
- Design for screws that anchor in print
  - Use modifier mesh to provide solid plastic for screw threads to bite into
  - Use plastic thread rolling screws (similar to wood screws)
    - Can be salvaged from old VCRs, stereos, microwave ovens, coffee makers, etc.
  - Size holes to fit screw tightly- it will make its own threads
Threaded brass insert
Thread rolling screw for plastic

---
Printed Registration Pins

---
Material Selection
- Consider:
  - Environmental factors- where will the print be kept or how will it be transported?
    - Moisture, temperature, sunlight (UV)
      - Post-print finishing may be necessary
  - Mechanical forces
    - Print strength depends on
      - Bed orientation
      - Wall, top and bottom thickness
      - Infill density
  - Light transmission
  - Difficulty of printing
    - Enclosed printer (ABS, maybe others)
    - Maximum bed and hot-end temperatures of the specific printer
    - Extruder nozzle material
      - Brass for most is OK
      - Steel, hardened steel, or ruby for abrasive (filled and GITD filaments) materials
  - Final appearance of the print
  - Cost and availability of the material

---
Additional Considerations
- 3D prints not inherently food-safe
  - Lead from brass nozzle is deposited in prints (?)
  - Small gaps between layers can’t be cleaned
  - Filament may contain harmful chemicals
  - Prints are usually not water-tight
- 3D prints can be used for a lot of things...
  - But not optimal for everything
- Post-print processing can fix a lot of problems